# Part 1- GENERAL

## REFERENCES

    - American Society for Testing and Materials (ASTM International)

    - ASTM A 653/A653M -Standard Specification for Steel Sheet, Zinc-Coated(Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process

    - ASTM D5796- Standard Test Method for Measurement of Dry Film Thickness of Thin-Film Coil-Coated Systems by Destructive Means Using a Boring Device

    - ASTM D5402 -Standard Practice for Assessing the Solvent Resistance of Organic Coatings Using Solvent Rubs, coating, curing characteristics, double rub method

    - ASTM D523-[Standard Test Method for Specular Gloss , appearance, directional reflectance factor, gloss, goniophotometry, high gloss, relative

    - ASTM D4145 -Standard Test Method for Coating Flexibility of Prepainted Sheet, coating flexibility, prepainted sheet, T-bend flexibility, Prepainted steel sheet

    - ASTM D4214- Standard Test Methods for Evaluating the Degree of Chalking of Exterior Paint Films, chalking, evaluation, exterior paint films

    - ASTM E330 – Standard Test Method for Structural Performace by Static Pressure Difference

    - ASTM G26- Practice for Operating Light-Exposure Apparatus (Xenon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials

1.1.2	American National Standarts Institute(ANSI)

-

ANSI B18.6.4-[99], Thread Forming and Thread Cutting Screws and Metallic Drive Screws.

1.1.2	Canadian General Standards Board (CGSB)

-	Metal Siding Standards : CAN/CGSB 93.4.92 & CAN/CGSB 93.5.92

## DESIGN REQUIREMENTS

    - Provide and install all the coverings of this section as well as the materials of all other siding.

    - The metal panels shall be designed to permit thermal contraction and expansion of the components due to temperature variations over a range of about 80°C, without excessive stress on the fastening devices, nor does it cause the buckling of the panels, the breaking of the seals or any other deterioration.

    - The maximum permissible deviation for the vertical and horizontal alignment of the panels in place is 1: 1000.

    - Harmonize and coordinate the work of metallic sidings with all contractors from all disciplines underlying and adjacent to the work of placing the panels.

    - The panel must withstand the seismic and wind loads found in the project area and meet the NBCC, 50-year probability (...kPa).

## TECHNICAL SPECS

    - Submit the required data sheets in accordance with section…(Documents and samples to be submitted).

    - Submit the technical data sheets of the wall covering system components. Specify the characteristics of the products, the colors chosen as well as the constraints and performance criteria to be respected.

## TECHNICAL DRAWINGS

    - Submit the required technical drawings in accordance with section…(Documents and samples to be submitted).

    - Indicate the dimensions and thickness of the panels, the anchoring and fixing methods, the location and details of the seals and joints, measurements to compensate for the contraction and thermal expansion movements, the planned openings in the walls, details of thresholds, supports, studs and lintels, materials and finishes, and requirements for calculation criteria and related work.

    - All technical drawings must be reviewed and approved by a verified and certified building structure Engineer in Quebec.

    - All documents must bear the seal of the structural engineer.

## SAMPLES

    - Submit the required data sheets in accordance with section…(Documents and samples to be submitted).

    - Submit to the site at the location designated by the architect a sample of two (2) panels of actual dimensions, with all moldings, reinforcements, inking system, sealing tape, fasteners, finish, colors and other. The production order will be accepted only after the architect has approved the sample.

## WORKFORCE QUALIFICATION

    - Metallic coverings must be installed by workers accredited by the manufacturer of the system used. The company that will install the metallic coverings must demonstrate by written documents, during the call for tenders, that it has a minimum of 5 years’ experience in commercial, institutional or industrial building envelope coverings.

## WARRANTIES

    - QUALITY GUARANTEES- The work referred to in this section is warranted by the installer against any defects in material or workmanship for a period of five years from the date of completion of the installation work.

    - MANUFACTURER'S WARRANTY - Provide a written warranty from the manufacturer against any defect in the exterior finish applied at the factory during the warranty period. The finish is guaranteed for 25 years after the near completion date. The values below are based on normal conditions and exclude any extraordinary atmospheric conditions.

The TEXTURAL IV paint system (PVDF base paint system) is guaranteed against cracking, peeling or loss of adhesion, visible to the naked eye within 10 meters for 40 years counting the date of application and according to the criteria of performance specifications of the manufacturer (paint applicator) and according to the conditions of the standard warranty of the manufacturer of the panels.

## STORAGE, HANDLING & TRANSPORTATION

    - Store and protect equipment and materials in accordance with manufacturer's recommendations for metal overlay panels.

    - Do not place or load with other products the top of the packages of the packed panels.

    - If the panels cannot be installed as soon as they are received, store them indoors in a dry, ventilated area.

    - If the panels are to be stored outdoors, place them away from direct sunlight, and protected from extreme temperatures (heat or cold). These extreme conditions can increase the adhesion of the protective film to panels, making it more difficult to remove and leave traces of glue on the panels after removal.

    - Do not leave unpacked and out of wooden brackets and packing boxes between installation work days.

## WASTE MANAGEMENT & DISPOSAL

    - Sort and recycle waste in accordance with the section (Construction Waste Management and Disposal).

    - Evacuate all packaging materials from the site and transport them to appropriate recycling facilities.

    - Recover and sort paper, plastic, polystyrene, corrugated cardboard. Packaging and place in appropriate waste bins disposed on site for recycling in accordance with the waste management plan.

    - Place in designated containers substances that meet the definition of toxic or hazardous waste.

    - It is prohibited to pour unused sealants into sewers, watercourses, lakes, the ground or any other place where there is a risk to health or the environment.

    - Route unused sealants to an approved hazardous materials collection site approved by the project manager.

    - Fold unused metal strips, flatten them and place them in designated areas for recycling.

# Part 2 - PRODUCTS

## MATERIALS & HARDWARE

    - Metal coverings:

      - Product of reference: (Harrywood) wall covering profile of manufacturer MAC (Metal Architectural) or equivalent approved by architect:

        - 6" (152 mm) center / center 0.34" (8.6 mm) deep;

        - In cut lengths of 144" (3658mm) and notched at the ends for longitudinal overlaying for pre-painted coatings in the colors of the wood collection;

      - Made of galvanized steel in accordance with ASTM 653M standard, 230 galvanized steel grades, 33 grade galvanized steel with zinc coating galvanized Z275 as designated by ASTM A653M.

      - Finish:

To be specified among the following WOOD COLLECTION 26-gauge choice of colours: Torrefied, Cedar, Black Walnut, Ash Grey, Smoked Birch, Scandinavian Fir

Each color specified must be made in 6 distinctive shades (with distinctive veining). The profiles made in this color will be packed in boxes of 12 panels of 12 linear feet in lenght including 2 panels of each distinctive shade. A packing box contains 72.75 sq. ft. of the Harrywood profile in 6 pre-mixed colors) The collection of WOOD colors is manufactured in accordance with the TEXTURAL IV pain system (base of the PVDF color system).

      - Nominal thickness

        - 0,46mm (gauge 26) for the color coatings of the wood collection

      - Starter moulding, valleys, gutters, transition mouldings and trim mouldings such as opening and protruding corner pieces, crown and drip flashings, starter tapes and opening trim in the same finish as the siding.

      - Fixations: Conform to the recommendations of the manufacturer MAC.

## ACCESSORIES

    - Concealed sealants:

      - ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

      - Meets ASTM C920, S, NS, Class 50, NT, M, GA, O

    - MAC visible sealants:

      - ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

      - Meets ASTM C920, S, NS, Class 50, NT, M, GA, O

    - Cold cutting equipment (Guillotine) specially designed by MAC for cutting Harrywood

    - Colour MAC retouching pencils to harmonize with the selected colour (…)

    - Fastening of the metal siding

      - Concealed mouldings : mouldings (except for sub-girts) and clips of TEXTURAL IV series crown flashings in pre-finished steel. Specify the same colour as HARRYWOOD siding from among the colours of the WOOD collection, in 26-gauge.

      - Standard manufacturer’s starter moulding #M10SHW in pre-finished steel designation G90

      - Continuous siding made of quality steel, zinc-coated with G90 design, 18-gauge, dimensions according to needs and site conditions.

      - Visible screws – Steel:

        - HWA 'POLYSEAL' TEK SCREW with sealing washer 8-18 x 1, 30618100YSP, visible screw, zinc appearance, visible moulding

Concealed screws – Wood:

        - <Jar200> VIS RD.WASH.VRX RT + QS ZC 8 x 1 1/8 <MAGNIS ARGENT W17> Incomplete thread.

#MJA41.0812PW17.20, concealed screw, zinc appearance, concealed moulding

Or

        - <Jar500> VIS RD.WASH.VRX RT + QS ZC 8 x 1 1/8 <MAGNIS ARGENT W17> Incomplete thread.

#MJA41.0812PW17.20, concealed screw, zinc appearance, concealed moulding

Concealed screws – Wood, unprotected:

        - Coarse thread wood screws type 17, round head / Vrex Zinc plug washer 8 x 1 1/8 VJA41.0812P.500

      - The screws must comply with CSA B11 and ANSI B18.6.4, respectively. These fasteners must be cadmium steel with flattened heads for concealed screws and hexagonal heads of the same colour as the panel equipped with a conical neoprene washer for visible screws.

      - See plans for all mouldings (standard mouldings for Harrywood siding) of the manufacturer to be used.

2.2.5.6 See plans for all non-standard mouldings (custom-made) and execute them according to the plans in pre-finished colours, 26-gauge (WOOD collection)

2.2.6	Any other accessories recommended by the manufacturer

# Part 3 - EXECUTION

## SUPPORT EVALUATION

Before proceeding with the installation of the siding panels and sheets, examine the support alignment and notify the architect in writing if the support does not meet the requirements of the panel installer. Before beginning to install the siding, ensure that your walls are square and level. Harrywood siding can be installed horizontally, vertically or diagonally.

## SIDING INSTALLATION

    - Tighten screws by applying moderate pressure to the metal to allow expansion. The screws must not exert any upward or downward pressure to avoid deforming the siding or opening the panels at the joints.

    - When joining the panels along their length, a space must be left for dilation and expansion of the material, depending on the temperature during installation.

    - Compliance: Comply with the manufacturer’s written requirements, recommendations, and specifications, including any available technical bulletins such as the installation guide, installation video sequences available on the manufacturer's web page, instructions in the product catalogue, those appearing on the packaging of the products, and the indications in the data sheets.

    - Install the starter strip, the interior corner (L-shaped steel corner, QJ trim interior corner), exterior corner (corner moulding, finished trim), window framing (adjustment, soffit J-trim), around the window outline (sides, top of the window), wall termination (adjustment, soffit J-trim). Refer to the installation guide on the manufacturer's website.

    - Install the exterior finish in accordance with the requirements of CGSB 93.5 and the manufacturer's written instructions.

    - Place the sub-girts, taking care to apply the thermal separator strips in continuity. Lay the furring so as to ensure continuous support for straight-level installation of the siding.

    - Before installing the siding, ensure that the walls are square and that the furrings (Z bars) are level.

    - Carefully lay the projecting corner pieces and adjacent moldings in order to obtain a well-shaped and profiled structure.

    - Provide and install shaped and waterproof fasteners for all system perimeters and perimeters of doors, shutters, and mechanical and electrical components to protect the walls from the elements. Ensure continuous pressure balance, according to the rain screen principle.

    - Lay the roof edges as shown.

    - Ensure that the siding joints are perfectly aligned and abutted.

    - Ensure that the Harrywood panels from the WOOD collection are placed randomly (at random, mixed over the height as well as the length in the case of long surfaces to cover). It is important never to reproduce the same installation sequence to harmonize the whole and avoid a “wallpaper” effect. NOTE: All the colours in the WOOD COLLECTION (Torrefied, Cedar, Black Walnut, Ash Grey, Smoked Birch, Scandinavian Fir) are available in six different panels of various wood grains and shades. Each of the panels is identified on the reverse side with a sequence of numbers from 1 to 6 in bold characters preceded by the # sign. The packing boxes contain 12 panels of six sq. ft. with premixed colours.

    - Cut the panels across the width only with the specialized tool (MAC SX14 Guillotine).

    - Cut (trim) panels to cold length only using scissors or electric scissors.

    - Caulk joints between adjacent elements and structures with a sealant / adhesive as specified in paragraphs 2.2.1 and 2.2.2

    - If there is a sealant overflow, be sure to clean the surplus immediately before it dries.

    - All Z bars on the exterior of the insulation are supplied and installed by the metal siding subcontractor.

## CLEANING

    - Follow the manufacturer's recommendations for panel maintenance and cleaning. Do not use solvents or chemicals.

    - Leave the work area clean and free from grease, stains, and finger marks.