# Part 1 – GENERAL

## REFERENCES

    - American Society for Testing and Materials (ASTM International)

      - ASTM A653 / A653M – Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process

      - ASTM D5796 – Standard Test Method for Measurement of Dry Film Thickness of Thin-Film Coil-Coated Systems by Destructive Means Using a Boring Device

      - ASTM D5402 – Standard Practice for Assessing the Solvent Resistance of Organic Coatings Using Solvent Rubs (coating, curing characteristics, double rub method)

      - ASTM D523 – Standard Test Method for Specular Gloss (appearance, directional reflectance factor, gloss, goniophotometry, high gloss, relative)

      - ASTM D4145 – Standard Test Method for Coating Flexibility of Prepainted Sheet (coating flexibility, prepainted sheet, T-bend flexibility, prepainted steel sheet)

      - ASTM D4214 – Standard Test Methods for Evaluating the Degree of Chalking of Exterior Paint Films (chalking, evaluation, exterior paint films)

      - ASTM E330 – Standard Test Method for Structural Performance by Static Pressure Difference

      - ASTM G26 – Practice for Operating Light-Exposure Apparatus (Xenon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials

1.1.2	American National Standards Institute (ANSI)

-

ANSI/ASME B18.6.4: 1999 Thread Forming and Thread Cutting Tapping Screws and Metallic Drive Screws

- Canadian General Standards Board (CGSB)

- Metal siding standards: CAN/CGSB 93.4.92 & CAN/CGSB 93.5.92

## DESIGN REQUIREMENTS

    - Provide and install all siding in this section as well as the materials of all other facings.

    - The metal panels shall be designed to allow thermal contraction and expansion of the components due to temperature variations over a range of about 80°C, without placing excessive stress on the fastening devices or causing buckling of the panels, breaking of the seals, or any other deterioration.

    - The maximum permissible deviation for the vertical and horizontal alignment of the panels in place is 1:1000.

    - Harmonize and coordinate the work of all metal siding contractors from all disciplines underlying and adjacent to the work of placing the panels.

    - Panels must withstand seismic and wind loads found in the project area and meet the CNBC 50-year probability (kPa).

## DATA SHEETS

    - Submit the required data sheets in accordance with section… (Documents and samples to be submitted).

    - Submit the data sheets of the siding system components. Specify the product features and selected colours, as well as the constraints and performance criteria to be respected.

## TECHNICAL DRAWINGS

    - Submit the required technical drawings in accordance with section… (Documents and samples to be submitted).

    - Indicate the dimensions and thickness of the panels, the anchoring and fastening methods, the location and details of the seals and joints, measures to compensate for thermal contraction and expansion movement, planned openings in the walls, details of thresholds, supports, studs and lintels, materials and finishes, and requirements for calculation criteria and related work.

    - All technical drawings must be reviewed and approved by a verified and certified building structure engineer in Québec.

    - All documents must bear the seal of the structural engineer.

## SAMPLES

    - Submit the required samples in accordance with section… (Documents and samples to be submitted).

    - Submit to the site at the location designated by the architect a sample of two (2) panels of actual dimensions, accompanied by all mouldings, reinforcements, anchoring system, sealing tape, fasteners, finish, colours, and other elements. The production order will be accepted only after the architect has approved the sample.

## WORKFORCE QUALIFICATION

    - Metal siding must be installed by workers accredited by the manufacturer of the system used. The company that will install the metal siding must demonstrate in writing during the call for tenders that it has a minimum of five years’ experience in commercial, institutional or industrial building siding.

## WARRANTIES

    - GUARANTEE OF QUALITY – The work referred to in this section is guaranteed by the installer against any defects in material or workmanship for a period of five years from the date of completion of the installation work.

    - MANUFACTURER’S WARRANTY – Provide a written warranty from the manufacturer against any defect in the exterior finish applied at the factory during the warranty period. The finish is guaranteed for 25 years following the substantial completion date. The values below are based on normal conditions and exclude any extraordinary atmospheric conditions.

The TEXTURAL IV paint system (PVDF-based paint system) is guaranteed against cracking, peeling or loss of adhesion visible to the naked eye within 10 metres for 40 years from the date of application and according to the criteria of the manufacturer’s performance specifications (paint applicator) and the conditions of the panel manufacturer’s standard warranty.

## STORAGE, HANDLING, AND TRANSPORTATION

    - Store and protect equipment and materials in accordance with the manufacturer’s recommendations for metal siding.

    - Do not place or load with other products on top of the packed panels.

    - If the panels cannot be installed as soon as they are received, store them indoors in a dry, ventilated area.

    - If the panels are to be stored outdoors, place them away from direct sunlight, protected from extreme temperatures (heat or cold). These extreme conditions can increase the adhesion of the protective film to panels, make it more difficult to remove, and leave traces of glue on the panels after removal.

    - Do not leave panels unpacked or out of their wooden brackets and packing boxes between installation work days.

## WASTE MANAGEMENT AND DISPOSAL

    - Sort and recycle waste in accordance with the section… (Construction Waste Management and Disposal).

    - Evacuate all packaging materials from the site and transport them to appropriate recycling facilities.

    - Recover and sort paper, plastic, polystyrene, and corrugated cardboard packaging and place in appropriate waste bins provided at the site for recycling in accordance with the waste management plan.

    - Place in designated containers substances that meet the definition of toxic or hazardous waste.

    - With approval of the project manager, send unused metal parts to a metal recycling facility.

    - It is prohibited to pour unused sealants into sewers, watercourses, lakes, the ground, or any other place where there is a risk to health or the environment.

    - With approval of the project manager, send unused sealants to a certified hazardous materials collection site.

    - Fold and flatten unused metal strips and place them in designated areas for recycling.

# Part 2 – PRODUCTS

## MATERIALS AND HARDWARE

    - Metal siding:

      - Reference product: (MS750) wall siding by MAC manufacturer (Metal Architectural) or equivalent approved by the architect:

        - Four longitudinal panels of raised point-type perforations

        - 20.375 in (518mm) siding width (covering area)

        - Customized lengths according to plans and specifications

        - 11/16 in (17.5mm) depth (panel thickness)

      - Made of galvanized steel in accordance with the ASTM 653M standard, 230 galvanized steel structural quality grade 33 with galvanized zinc Z275 coating as designated by ASTM A653M

      - Finish

To be specified among the following:

- The SIGNATURE COLLECTION in 24-gauge, including the colours BRUSHED ZINC, QUARTZ ZINC, ANTHRACITE ZINC, and RENAISSANCE BRONZE, is manufactured in accordance with the TEXTURAL IV paint system (PDVF-based colour system).

- The SIGNATURE WOOD COLLECTION is manufactured in accordance with the TEXTURAL IV paint system (PVDF- based colour system).

- The INSPIRATION COLLECTION in 24-gauge, including the colours TITANIUM BLACK, TITANIUM WHITE, and METALLIC GREY is manufactured in accordance with the TEXTURAL III paint system (polyurethane-based system).

      - Nominal thickness

- 0.46 mm (26-gauge) for the WOOD COLLECTION colour coatings

- 0.61 mm (24-gauge) for the SIGNATURE and INSPIRATION COLLECTIONS colour coatings

      - Starter moulding, valleys, gutters, transition mouldings and trim mouldings such as opening and protruding corner pieces, crown and drip flashings, starter tapes and opening trim in the same finish as the siding

      - Fastenings: Compliant with the recommendations of the MAC manufacturer

## ACCESSORIES

    - Concealed sealants:

      - ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

      - Meets ASTM C920, S, NS, Class 50, NT, M, GA, O 2.2.2 Apparent sealing compounds from MAC

      - ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

      - Meets ASTM C920, S, NS, Class 50, NT, M, GA, O

    - Cold cutting equipment (Guillotine) specially designed by MAC for cutting Norwood MS750.

    - Colour MAC retouching pencils to harmonize with the TORRIFIED colour.

    - Fastening of the metal siding

      - Concealed mouldings: mouldings (except for sub-girts) and clips of TEXTURAL IV or TEXTURAL III series crown flashings in pre-finished steel. Specify the same colour as NORWOOD siding from among the colours of the SIGNATURE or INSPIRATION collections, in 26-gauge.

      - Standard manufacturer’s starting moulding.

      - Continuous siding made of quality steel, zinc-coated G90 designation, 18-gauge, dimensions according to needs and site conditions.

Visible screw – Steel:

HWA ‘POLYSEAL’ TEK SCREW with sealing washer 8-18 x 1, 30618100YSP, visible screw, zinc appearance, visible moulding

Visible screw – Wood:

-		‘POLYSEAL’ TOLE SCREW with sealing washer 9 x 1, 30409100YSP, wood visible screw, zinc appearence, coloured or plain

      - The screws must comply with CSA B11 and ANSI B18.6.4, respectively. These fasteners must be cadmium steel with flattened heads for concealed screws and hexagonal heads of the same colour as the panel equipped with a conical neoprene washer for visible screws.

      - See plans for all mouldings (standard mouldings for Norwood siding) of the manufacturer to be used.

      - See plans for all non-standard mouldings (custom-made) and execute them according to the plans in pre- finished colours, 26- or 24-gauge (SIGNATURE or INSPIRATION collection).

2.2.6 Any other accessories recommended by the manufacturer

# Part 3 – EXECUTION

## SUPPORT EVALUATION

3.1.1 Before proceeding with the installation of the siding panels and sheets, examine the support alignment and notify the architect in writing if the support does not meet the requirements of the panel installer.

## SIDING INSTALLATION

Before beginning to install the siding, ensure that your walls are square and level. MS 750 wall siding can be installed horizontally, vertically or diagonally.

    - Tighten screws by applying moderate pressure to the metal to allow expansion. The screws must not exert any upward or downward pressure to avoid deforming the siding or opening the panels at the joints.

    - When joining the panels along their length, a space must be left for dilation and expansion of the material, depending on the temperature during installation.

    - Compliance: Comply with the manufacturer’s written requirements, recommendations, and specifications, including any available technical bulletins such as the installation guide, installation video sequences available on the manufacturer's web page, instructions in the product catalogue, those appearing on the packaging of the products, and the indications in the data sheets.

    - Install the exterior finish in accordance with the requirements of CGSB 93.5 and the manufacturer's written instructions.

    - Lay the furring so as to ensure continuous support for straight-level installation of the siding. Furring at intervals of 16 to 24 inches.

    - Continuous installation of drip mouldings, starter mouldings, entrance / exit corner pieces, curbs, soffits, mouldings adjacent to doors and windows, according to manufacturer's prototypes and recommendations.

    - The SOFFITE panels (MS750) are assembled by partial superimposition (first valley of the panel to be placed over the last valley of the previously installed panel). The face is in line with sealing washer screws at the bottom of each second panel valley (= 5 screws visible per panel at the level of the girts).

    - Place the sub-girts, taking care to apply the thermal separator strips in continuity. Lay the furring so as to ensure continuous support for straight-level installation of the siding.

    - Before installing the siding, ensure that the walls are square and that the furrings (Z bars) are level.

    - Carefully lay the projecting corner pieces and adjacent moldings in order to obtain a well-shaped and profiled structure.

    - Provide and install shaped and waterproof fasteners for all system perimeters and perimeters of doors, shutters, and mechanical and electrical components to protect the walls from the elements. Ensure continuous pressure balance, according to the rain screen principle.

    - Lay the roof edges as shown.

    - Ensure that the siding joints are perfectly aligned and abutted.

    - Cut (trim) panels to cold length only using scissors or electric scissors.

    - Caulk joints between adjacent elements and structures with a sealant /adhesive as specified in paragraphs

2.2.1 and 2.2.2

    - If there is a sealant overflow, be sure to clean the surplus immediately before it dries.

    - All Z bars on the exterior of the insulation are supplied and installed by the metal siding subcontractor.

## CLEANING

    - Follow the manufacturer's recommendations for panel maintenance and cleaning. Do not use solvents or chemicals.

    - Leave the work area clean and free from grease, stains, and finger marks.