GENERAL

REFERENCES

American Society for Testing and Materials (ASTM International)

ASTM A653/A653M - Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process

ASTM D5796 - Standard Test Method for Measurement of Dry Film Thickness of Thin-Film Coil-Coated Systems by Destructive Means Using a Boring Device

ASTM D5402 - Standard Practice for Assessing the Solvent Resistance of Organic Coatings Using Solvent Rubs, coating, curing characteristics, double rub method

ASTM D523 - Standard Test Method for Specular Gloss, appearance, directional reflectance factor, gloss, goniophotometry, high gloss, relative

ASTM D4145 - Standard Test Method for Coating Flexibility of Prepainted Sheet, coating flexibility, prepainted sheet, T-bend flexibility, Prepainted steel sheet

ASTM D4214 - Standard Test Methods for Evaluating the Degree of Chalking of Exterior Paint Films, chalking, evaluation, exterior paint films

ASTM G26 - Practice for Operating Light-Exposure Apparatus (Xenon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials

ASTM E84 - Standard Test Method for Surface Burning Characteristics of Building Materials

ASTM E2768 - Standard Test Method for Extended Duration Surface Burning Characteristics of Building Materials (30 min Tunnel Test)

ASTM B117 - Standard Practice for Operating Salt Spray (Fog) Apparatus

ASTM G85 - Standard Practice for Modified Salt Spray (Fog) Testing

ASTM D2247 - Standard Practice for Testing Water Resistance of Coatings in 100 % Relative Humidity

ASTM D2244 - Standard Practice for Calculation of Color Tolerances and Color Differences from Instrumentally Measured Color Coordinates

ASTM D3363 - Standard Test Method for Film Hardness by Pencil Test

American National Standards Institute (ANSI)

ANSI B18.6.4-[99], Thread Forming and Thread Cutting Screws and Metallic Drive Screws.

Canadian Sheet Steel Building Institute (CSSBI)

Standard for Residential Steel Cladding: CSSBI 23M-16

CAN/CGSB 93.3.92 & CAN/CGSB 93.4.92

CAN/ULC

CAN/ULC-S135 Heat Release Test

CAN/CSA

CAN/CSA-S136-16 (R2021) North American specification for the design of cold-formed steel structural members

Wildland Urban Interface (WUI)

Inscription 8140-2358-0500 (MS3 only)

DESIGN REQUIREMENTS

Provide and install all the coverings of this section as well as the materials of all other siding.

The metal panels shall be designed to permit thermal contraction and expansion of the components due to temperature variations over a range of about 80°C, without excessive stress on the fastening devices, nor does it cause the buckling of the panels, the breaking of the seals or any other deterioration.

The maximum permissible deviation for the vertical and horizontal alignment of the panels in place is 1: 1000.

Harmonize and coordinate the work of metallic sidings with all contractors from all disciplines underlying and adjacent to the work of placing the panels.

The panel must withstand the seismic loads and wind pressure found in the project area and meet the NBCC, 50-year probability (…kPa). Refer to MAC Metal Architectural test reports and certifications document on the website for test data.

TECHNICAL SPECS

Submit the required data sheets in accordance with section… (Documents and samples to be submitted).

Submit the technical data sheets of the wall covering system components. Specify the characteristics of the products, the colours chosen as well as the constraints and performance criteria to be respected.

TECHNICAL DRAWINGS

Submit the required technical drawings in accordance with section… (Documents and samples to be submitted).

Indicate the dimensions and thickness of the panels, the anchoring and fixing methods, the location and details of the seals and joints, measurements to compensate for the contraction and thermal expansion movements, the planned openings in the walls, details of thresholds, supports, studs and lintels, materials and finishes, and requirements for calculation criteria and related work.

All technical drawings must be reviewed and approved by a verified and certified building structure Engineer in your locality. MAC Metal Architectural does not offer building engineering services and any recommendation or advice given must not be taken as a construction directive.

All documents must bear the seal of the structural engineer.

SAMPLES

Submit the required data sheets in accordance with section… (Documents and samples to be submitted).

Submit to the site at the location designated by the architect a sample of two (2) panels of actual dimensions with all moldings, reinforcements, inking system, sealing tape, fasteners, finish, colours and other. The production order will be accepted only after the architect has approved the samples and colours.

WORKFORCE QUALIFICATION

Metallic coverings must be installed by workers accredited by the manufacturer of the system used. The company that will install the metallic coverings must demonstrate by written documents, during the call for tender, that it has a minimum of 5 years experience in commercial, institutional of industrial building envelope coverings.

WARRANTIES

QUALITY & INSTALLATION GUARANTEES - The work referred to in this section is warranted by the installer against any defects in material or workmanship for a period of five years from the date of completion of the installation work.

MANUFACTURER'S WARRANTY - Provide a written warranty from the manufacturer against any defect in the exterior finish applied at the factory during the warranty period. The finish is guaranteed for 40 years after the near completion date. This is based on normal conditions and excludes any extraordinary atmospheric or environmental conditions leading to premature defects. Refer to the MAC warranty document for all details. There is no finish warranty on product corrosion. Although painted galvanized steel finish will corrode slowly, edge creep can begin to show typically within the first 5-15 years. Proper cutting methods and edge protection during installation will help slow edge creep and application of touch up paint on the cut edges will delay corrosion.

Use best practices installation methods of the steel panel and accessory products and ensure compliance with local code. Manufacturer installation guides and videos should be reviewed before moving forward with installation. Steel shape variation, wall straightness, screw angles and pressure applied on the panel will all factor in the finish quality of the building envelope. Some oil canning may remain even on proper installation due to the nature of steel panels.

STORAGE, HANDLING & TRANSPORTATION

Store and protect equipment and materials in accordance with manufacturer's recommendations for metal siding panels.

Do not place or load with other products the top of the packages of the MAC panels.

If the panels cannot be installed as soon as they are received, store them indoors in a dry, ventilated area, especially if storing MS series or any other products using foam separators as this may stain the paint if improperly stored.

If the panels are to be stored outdoors, place them away from direct sunlight, and protected from extreme temperatures (heat or cold). These extreme conditions can increase the adhesion of the protective film to panels, making it more difficult to remove and leave traces of glue on the panels after removal. They should be stored in a way that rain and moisture do not come in contact with the product.

Do not leave unpacked panels and out of wooden skids and packing boxes between installation workdays.

WASTE MANAGEMENT & DISPOSAL

Sort and recycle waste in accordance with the section (Construction Waste Management and Disposal).

Evacuate all packaging materials from the site and transport them to appropriate recycling facilities.

Recover and sort paper, plastic, polystyrene, corrugated cardboard packaging and place in appropriate waste bins disposed on site for recycling in accordance with the waste management plan.

Place in designated containers substances that meet the definition of toxic or hazardous waste.

It is prohibited to pour unused sealants into sewers, watercourses, lakes, the ground or any other place where there is a risk to health or the environment.

Route unused sealants to an approved hazardous materials collection site approved by the project manager.

Fold unused metal strips, flatten them and place them in designated areas for recycling.

PRODUCTS

MATERIALS & HARDWARE

Metal coverings :

Product of reference: MS3 and MS4 roof covering profiles of manufacturer MAC Metal Architectural or equivalent approved by architect:

17.75" (450.9 mm) center / center, 1-1/2" (38.1 mm) deep.

In custom cut lengths ranging from 3’ to 60’ according to plans and specifications.

Made of galvanized steel in accordance with ASTM 653M standard, 33 SS grade (230 MPa) galvanized steel with zinc coating galvanized G90 (Z275) as designated by ASTM A653M.

Finish:

- Pre-finished steel, G90 (Z275)

SIGNATURE and INSPIRATION colour collections

TEXTURAL II (SMP-based), TEXTURAL III (Polyurethane-based) and TEXTURAL IV (PVDF-based) paint systems

Nominal thickness

0.46 mm (26-gauge)

Accessories: Starter moulding, valleys, gutters, transition mouldings and trim mouldings such as opening and protruding corner pieces, crown and drip flashing, starter tapes and opening trim in the same finish as the siding.

Fixations: Follows local regulation & Code. Professional in charge of the project to consider payload and dynamic load of wind applied on the profile. Minimum thickness of girts to respect the manufacturer recommendation.

ACCESSORIES

Concealed sealants

ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

Meets ASTM C920, S, NS, Class 50, NT, M, GA, O

Meets ASTM C1184 for two-sided structural glazing

Meets AAMA 802 and 805 standards

Meets American Federal Specifications TT-S-1543A, class A and TT-S-00230C, class A, type I

CFIA accepted

UL 2818 GREENGUARD and GREENGUARD GOLD certification

Complies with FDA 21CFR177.2600 (indirect contact / open joint)

Or equivalent

Exposed Sealants

In compliance with [Section 079200]

Approved saw blade in good working condition; refer to website for approved cold cut low temperature blades; extra precaution to be taken on blade quality and generated temperature to ensure it doesn’t damage the galvanization and paint layers.

Colour MAC retouching pencils to harmonize with the selected colour (…)

Fastening of the metal siding

Concealed mouldings: mouldings (except for sub-girts) and clips of TEXTURAL IV series crown flashings in pre-finished steel. Specify the same colour as MS3 / MS4 siding from among the colours of the SIGNATURE and INSPIRATION.

Sub-girts (Z-bar or Omega) of quality steel, zinc-coated with G90 design, 16 to 22 gauge or as per sub wall assembly structure requirement, dimensions according to needs and site conditions.

Concealed screws - Wood :

A058.250; screw model supplied by MAC

- Wood screw, 1-1/4" length, coarse thread type 17, round head with integrated washer concealed screw, zinc appearance with corrosion protection finish, concealed moulding.

- OR

Concealed screws – Metal :

A063.250; screw model supplied by MAC

- Self-drilling (Tek) metal screw, 1-1/4" length, coarse thread type 17, round head with integrated washer concealed screw, zinc appearance with corrosion protection finish, concealed moulding.

The screws must comply with CSA B11 and ANSI B18.6.4, respectively. These fasteners must be cadmium steel with flattened heads for concealed screws and hexagonal heads of the same colour as the panel equipped with a conical neoprene washer for visible screws.

See plans for all mouldings (standard mouldings for MS3 / MS4) of the manufacturer to be used.

See plans for all non-standard mouldings (custom-made) and execute them according to the plans in pre-finished colours.

Any other accessories recommended by the manufacturer.

EXECUTION

SUPPORT EVALUATION

Before proceeding with the installation of the siding panels and sheets, examine the support alignment and notify the architect in writing if the support does not meet the requirements of the panel installer. Before beginning to install the siding, ensure that your walls are square and level. MS3 and MS4 roofings can only be installed vertically.

ROOFING INSTALLATION

Tighten screws by applying moderate pressure to the metal to allow for expansion. The screws must not exert any upward or downward pressure to avoid deforming the roofing or opening the panels at the joints.

When joining the panels along their length, a space must be left for dilation and expansion of the material, depending on the temperature during installation. Consult the MAC installation guides for recommended minimum gap in between the panels, moldings and accessories.

Comply with the manufacturer’s written requirements, recommendations, and specifications, including any available technical bulletins such as the installation guide, installation video sequences available on the manufacturer's web page, instructions in the product catalogue, those appearing on the packaging of the products, and the indications in the data sheets.

Lay plywood sheets with a minimum thickness of 5/8” in order to provide uniform support for the installation of the metal facings and ensure a level installation.

Install an undercoating system of the MAC self-adhesive membrane roof (LASTOBOND SHIELD type from SOPREMA) or equivalent to receive metal roofing according to the manufacturer's recommendations.

In the case of metal furring (Z bars of 18 or 20 gauge), the continuous furring must be laid in such a way as to provide support for the installation of the facing and to ensure a level installation.

Continuous mouldings, ridges, valleys, and sloping mouldings must be installed on the walls according to the manufacturer's instructions.

Install the exterior finish in accordance with the requirements of CGSB 93.5 and the manufacturer's written instructions.

The roofing must be clipped after the initial mouldings and valleys according to the manufacturer's instructions. The ends of the panels are folded with a manual folding tool (MAC) while the ends of the clips are cut and closed by hand.

Before clipping the panels after the valleys, it is recommended by the manufacturer to apply two lines of sealant all along the surface of the extreme wings of the valleys.

When working in the valley section, close the clips and clip the panel in the valley.

For low-slope roof application, snow retention areas and valley sections, MAC sealant must be applied inside the groove on the male side of the valley, as recommended by the manufacturer. Clip before nesting the panels and seal the panels on the exterior near the joints, creating a transition with the valleys to prevent water infiltration due to the hydrostatic pressure of wet snow or ice.

The ventilated or unventilated ridge caps are placed first and the roof panels, whose ends are shaped in advance on the site are slid inside their pockets (turned upward and sealed next to the clips) as recommended by the manufacturer. Seal the backs of the ends of the roof panels where they finish up in the ventilated or unventilated pocket using MAC sealant or equivalent.

Caulk joints between adjacent elements and structures with a sealant / adhesive as specified in paragraphs 2.2.1 and 2.2.2 OR equivalent.

If there is a sealant overflow, be sure to clean the surplus immediately before it dries on the panels or trims.

Install sealants at junctions with adjoining work and where shown on the drawings in accordance with Section [079200-Sealants] for Adfast Sealant only.

Provide and install shaped and waterproof fasteners for all system perimeters and perimeters of doors, shutters, and mechanical and electrical components to protect the walls from the elements. Ensure continuous pressure balance, according to the rain screen principle.

Use colour matched touch-up paint to touch-up any installation defect. A good installation practice is to touch-up any cut edge.

All metal girts or sub-structure on the exterior of the insulation are supplied and installed by the metal siding subcontractor.

CLEANING

Follow the manufacturer's recommendations for panel maintenance and cleaning. Do not use solvents or chemicals unless previously approved by the manufacturer as it may void the paint warranty. If not only using mild soap and water for cleaning, only the products in the “Maintenance of the profiles” paper are approved by the manufacturer.

Leave the work area clean and free from grease, stains, and finger marks.