# Part 1 – GENERAL

## REFERENCES

    - American Society for Testing and Materials (ASTM International)

      - ASTM A653 / A653M – Standard Specification for Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process

      - ASTM D5796 – Standard Test Method for Measurement of Dry Film Thickness of Thin-Film Coil-Coated Systems by Destructive Means Using a Boring Device

      - ASTM D5402 – Standard Practice for Assessing the Solvent Resistance of Organic Coatings Using Solvent Rubs (coating, curing characteristics, double rub method)

      - ASTM D523 – Standard Test Method for Specular Gloss (appearance, directional reflectance factor, gloss, goniophotometry, high gloss, relative)

      - ASTM D4145 – Standard Test Method for Coating Flexibility of Prepainted Sheet (coating flexibility, prepainted sheet, T-bend flexibility, prepainted steel sheet)

      - ASTM D4214 – Standard Test Methods for Evaluating the Degree of Chalking of Exterior Paint Films (chalking, evaluation, exterior paint films)

      - ASTM E330 – Standard Test Method for Structural Performance by Static Pressure Difference

      - ASTM G26 – Practice for Operating Light-Exposure Apparatus (Xenon-Arc Type) With and Without Water for Exposure of Nonmetallic Materials

    - American National Standards Institute (ANSI)

-

ANSI/ASME B18.6.4-[99] – Thread Forming and Thread Cutting Tapping Screws and Metallic Drive Screws

    - Canadian General Standards Board (CGSB)

-	Metal siding standards: CAN/CGSB 93.4.92 & CAN/CGSB 93.5.92

## QUALITY INSURANCE

    - The manufacturer and installer of metal roofing and siding must demonstrate experience in carrying out projects of a similar size.

    - This section establishes the quality standards for the installation of MAC metal siding. Any substitution must meet this standard and will be subject to the following requirements:

      - An application for authorization of a substitution must be made in writing and received at least ten (10) days before the closing date of the call for tenders.

      - The application shall include a detailed item-by-item comparison of the proposed substitution and the specified system and shall be accompanied by relevant manufacturer documentation, samples, test data, and identical technical standards, or with a yield above the specified standards.

## DESIGN REQUIREMENTS

    - Provide and install all siding in this section as well as the materials of all other facings.

    - The metal panels shall be designed to allow thermal contraction and expansion of the components due to temperature variations over a range of about 80°C, without placing excessive stress on the fastening devices or causing buckling of the panels, breaking of the seals, or any other deterioration.

    - The maximum permissible deviation for the vertical and horizontal alignment of the panels in place is 1:1000.

    - Harmonize and coordinate the work of all metal siding contractors from all disciplines underlying and adjacent to the work of placing the panels.

    - The roof must be resistant to seismic loads and positive or negative wind loads expected in the geographic area of project implementation (CNBC 50-year probability [kPa]).

    - The roof must be able to withstand overloads due to snow accumulations and rain expected in the geographic area of project implementation (CNBC 50-year probability [kPa]).

    - In the case of a roof or wall installation, the roof system (wall) must not deflect more than 1/240 (1/180) of the bearing surface for loads due to wind and snow conditions limits of functionality.

    - The roof must be designed to withstand its own load.

    - The roof must be designed to have a minimum slope of 10 degrees for pre-finished siding in the TEXTURAL III paint system and 15 degrees for pre-finished siding in the TEXTURAL IV paint system.

## DATA SHEETS

    - Submit the required data sheets in accordance with section… (Documents and samples to be submitted).

    - Submit the data sheets of the roofing (wall) system components. Specify the product features and selected colours, as well as the constraints and performance criteria to be respected.

  - TECHNICAL DRAWINGS

1.5.1 Submit the required technical drawings in accordance with section… (Documents and samples to be submitted).

    - Indicate the dimensions and thickness of the panels, the anchoring and fastening methods, the location and details of the seals and joints, measures to compensate for thermal contraction and expansion movement, planned openings in the walls, details of thresholds, supports, studs and lintels, materials and finishes, and requirements for calculation criteria and related work.

    - All technical drawings must be reviewed and approved by a verified and certified building structure engineer in Québec.

    - All documents must bear the seal of the structural engineer.

## SAMPLES

    - Submit the required samples in accordance with section… (Documents and samples to be submitted).

    - Submit to the site at the location designated by the architect a sample of two (2) panels of actual dimensions, accompanied by all mouldings, reinforcements, anchoring system, sealing tape, fasteners, finish, colours, and other elements. The production order will be accepted only after the architect has approved the sample.

## WORKFORCE QUALIFICATION

    - Metal siding must be installed by workers accredited by the manufacturer of the system used. The company that will install the metal siding must demonstrate in writing during the call for tenders that it has a minimum of five years’ experience in commercial, institutional or industrial building siding.

## LABOUR QUALITY WARRANTY

    - The work referred to in this section is guaranteed by the installer against any defects in material or workmanship for a period of 10 years from the date of completion of the installation work.

## STORAGE, HANDLING, AND TRANSPORTATION

    - Store and protect equipment and materials as recommended by the panel manufacturer.

    - Do not expose panels to extreme heat.

    - Do not place or load with other products on top of the packed panels.

    - Do not leave panels unpacked or out of their wooden brackets and packing boxes between installation work days.

    - Ensure the protection of pre-finished steel during manufacture, transportation, on-site storage, and installation in accordance with CSSBI standards.

## MAINTENANCE DATA

1.10.1 Provide maintenance and cleaning data for panel finishes for inclusion in the manual specified in Section…

## MANUFACTURER WARRANTY

    - Provide a written warranty from the panel manufacturer against any defect in the exterior finish applied at the factory during the warranty period. The finish is guaranteed for 40 years (depending on the colour choice and paint system).

## WASTE MANAGEMENT AND DISPOSAL

1.12.1 Sort and recycle waste in accordance with the section… (Construction Waste Management and Disposal).

    - Evacuate all packaging materials from the site and transport them to appropriate recycling facilities.

    - Recover and sort paper, plastic, polystyrene, and corrugated cardboard packaging and place in appropriate waste bins provided at the site for recycling in accordance with the waste management plan.

    - Place in designated containers substances that meet the definition of toxic or hazardous wastes.

    - With approval of the project manager, send unused metal parts to a metal recycling facility.

    - It is prohibited to pour unused sealants into sewers, watercourses, lakes, the ground, or any other place where there is a risk to health or the environment.

    - With approval of the project manager, send unused sealants to a certified hazardous materials collection site.

    - Fold and flatten unused metal strips and place them in designated areas for recycling.

Part 2 – PRODUCTS

## MATERIALS AND HARDWARE

    - Steel roofing and siding:

      - Reference product: (MS1 / MS2) metal siding by MAC manufacturer (Metal Architectural) or equivalent approved by architect:

- 19.20 in (488 mm) centre / centre

      - Finish:

TEXTURAL III series pre-finished steel (polyurethane-based colour system) MHQC colour… or TEXTURAL IV series (PVDF-based colour system) MHQC colour

      - Nominal thickness

- 0.46 mm (26- gauge) or 0.61 mm (24-gauge)

      - Provide exterior panels and metal facings as well as the longest possible accessories to minimize the number of joints.

      - Starter moulding, valleys, gutters, transition mouldings and trim mouldings such as opening and protruding corner pieces, crown and drip flashings, starter tapes and opening trim in the same finish as the siding

      - Fasteners: Compliant with the recommendations of the MAC manufacturer

      - Dimensions of the panels: See drawings for measurements.

## 2.2	ACCESSORIES

    - Concealed sealants:

- ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

- Meets ASTM C920, S, NS, Class 50, NT, M, GA, O

    - Visible sealants:

- ADSEAL DWS 4580 SERIES (NEUTRAL SILICONE ADHESIVE SEALANT PERIMETER JOINTS)

- Meets ASTM C920, S, NS, Class 50, NT, M, GA, O

    - MAC (Metal Architectural) manual folding tool for partial folding of the ends of MS1 / MS2 panels

    - MAC retouching pencils (Metal Architectural assorted colours from the TEXTURAL III series)

    - Fastening of the steel siding

      - VIS LATTÉ “S” 8 x 1 ¼ PHOS 8 x 1 ¼ (31228114-1VN), K-LATCH for non-visible mouldings, quality steel continuous siding, zinc plated with G90 design, pre-finished in TEXTURAL III paint system Or TEXTURAL IV as well as for Galvalume continuous steel siding mounted on wood girts

      - VIS LATTÉ TEK ‘POLYSEAL’ 8-18 X 1 ¼ (31228114Y) for non-visible mouldings, high-quality continuous steel siding, zinc plated with G90 design, pre-finished in TEXTURAL III paint system Or TEXTURAL IV as well as for Galvalume continuous steel profiles mounted on steel sub-girders.

      - The screws must comply with CSA B11 and ANSI B18.6.4, respectively. These fasteners must be cadmium steel with flattened heads for concealed screws and hexagonal heads of the same colour as the panel equipped with a conical neoprene washer for visible screws.

      - The screws must be treated with a high-solids, single component, aluminum-containing, high-solubility polyurethane primer in accordance with ASTM B117 (6703 Liquigalv: 3,000hrs and 6704 aluminum primer: 2,000 hrs).

      - See plans for all standard mouldings of the manufacturer to be used.

    - Any other accessories recommended by the manufacturer

# Part 3 – EXECUTION

## SUPPORT EVALUATION

    - Before proceeding with the installation of the siding panels and sheets, examine the support alignment and notify the architect in writing if the support does not meet the requirements of the panel installer.

## INSTALLATION

    - Compliance: Comply with the manufacturer’s written requirements, recommendations, and specifications, including any available technical bulletins instructions in the product catalogue, those appearing on the packaging of the products, and the indications in the data sheets.

    - Install the exterior finish in accordance with the requirements of CGSB 93.5 and the manufacturer's written instructions.

    - Lay plywood sheets with a minimum thickness of 5/8 in order to provide uniform support for the installation of the metal facings and ensure a level installation.

    - Install an undercoating system of the MAC self-adhesive membrane roof (LASTOBOND SHIELD type from SOPREMA) or equivalent to receive metal siding according to the manufacturer's recommendations.

    - In the case of metal furring (Z bars of 18- or 20-gauge), the continuous furring must be laid in such a way as to provide support for the installation of the facing and to ensure a level installation.

    - For roofing applications, continuous mouldings, ridges, valleys, and sloping mouldings must be installed on the walls according to the manufacturer's instructions.

    - For wall-mounted applications, fit the corner fittings, curbs, flaps, flashings, threshold, and support fittings, as well as window and door window flashings and fittings as indicated.

    - Carefully position the protruding corner pieces, filler pieces and closing parts to obtain a well-shaped and profiled structure.

    - In the case of a roof application, the siding must be clipped after the initial mouldings and valleys according to the manufacturer's instructions. The ends of the panels are folded with a manual folding tool (MAC) while the ends of the clips are cut and closed by hand.

    - Before clipping the panels after the valleys, it is recommended by the manufacturer to apply two lines of sealant all along the surface of the extreme wings of the valleys.

    - When working in the valley section, close the clips and clip the panel in the valley.

    - For low-slope roof application, snow retention areas and valley sections, MAC sealant must be applied inside the groove on the male side of the valley, as recommended by the manufacturer. Clip before nesting the panels and seal the panels on the exterior near the joints, creating a transition with the valleys to prevent water infiltration due to the hydrostatic pressure of wet snow or ice.

    - Secure the elements so as not to impede thermal movements of contraction and expansion.

    - In the case of a roof application, the ventilated or unventilated ridge caps are placed first and the roof panels, whose ends are shaped in advance on the site are slid inside their pockets (turned upward and sealed next to the clips) as recommended by the manufacturer. Seal the backs of the ends of the roof panels where they finish up in the ventilated or unventilated pocket using MAC sealant or equivalent.

    - Caulk joints between adjacent elements and structures with a high performance, solvent-free, isocyanate-free, non-yellowing, MAC-elastomer sealant, Type S, NS Grade, Class 25 and AAMA 802 802.3 Type of Bedding compound. UL723 accredited. USDA agreed.

    - Clip systems: Fasten the panels using fasteners as recommended by the manufacturer and according to the manufacturer's method of installation. Use concealed fasteners for siding and mouldings. Exposed fixings must be minimized and match the roof.

    - Repair minor surface defects using a high-quality retouching pen in a colour that matches the colour of the panel (the architect must authorize the retouching and approve the result).

    - Replace damaged panels and components that, in the opinion of the architect, cannot be repaired correctly.

## CLEANING

    - Leave the work area clean and free from grease, stains, and finger marks.

    - Remove excess sealant with the recommended solvent.

    - Clean the exposed surfaces of the panels according to the manufacturer's instructions.